CLASSIFICATION AND DESCRIPTION OF ENGINEERING SOILS

Soil Classification

The object of soil classification is to provide a basis where engineers can group soils according to their physical characteristics and appearance for the purposes of comparing different soils, communicating their properties and to a limited extent assessing their suitability for particular engineering use.  The physical characteristics and appearance of a granular soil are influenced mainly by the distribution of various particle sizes in the soil deposit and of a clay soil cohesion and plasticity properties associated with its mineralogical composition of water content and also by its natural microstructure.  The granular fraction of a soil deposit is therefore classified according to its particle size distribution while the clay fraction is classified according to its plasticity characteristics in terms of what are known as its Atterberg limits.

Particle Size Distribution

The distribution of particle in a soil mass is usually expressed in terms of a grading curve or a particle size distribution curve in which the percentage by mass of particles finer than any particle size is plotted against particle size to a logarithmic scale.  The sand and gravel fractions are graded according to the sieve analysis and the silt fraction according to the sedimentation analysis.

Sieve analysis: A representative sample of soil of known mass is passed through a series of standard sieves havng successively finer aperture size and the mass of soil retained on each sieve is measured.  This enables the cumulative percentage by mass of the soil sample passing through each sieve to be calculated and plotted against the relevant aperture size.  The range of test sieves commonly used for particle size analysis is given according to the British and American standards below:

| British Standard |  | ASTM Standard |  |
| --- | --- | --- | --- |
| 75 | mm | 75 | mm |
| 63 |  | 50 |  |
| 50 |  | 37.5 |  |
| 37.5 |  | 25 |  |
| 28 |  | 19 |  |
| 20 |  | 9.5 |  |
| 14 |  | 4.75 |  |
| 10 |  | 2.36 |  |
| 6.3 |  | 2 |  |
| 5 |  | 1.18 |  |
| 3 |  | 850 | µm |
| 35 |  | 600 |  |
| 2 |  | 425 |  |
| 1.18 |  | 300 |  |
| 600 | µm | 250 |  |
| 425 |  | 150 |  |
| 300 |  | 106 |  |
| 212 |  | 75 |  |
| 150 |  |  |  |

If the soil contains silt and clay size particles the sample is first treated with a deflocculating agent and washed through selected sieves to isolate the fines.  The coarse grain material is then dried and sieved using the sieve analysis.

Sedimentation analysis: The size of silt particles places them beyond the practical limit of sieve analysis and so the size distribution over the silt range is determined by observing the sedimentation characteristics of the particles as they settle out of suspension in water.  The sedimentation analysis is carried out on material which has passed through the 63 µm British Standard sieve.  A suspension of known concentration is prepared using distilled water to which a deflocculating agent has been added to ensure that the particles settle out separately.  After being thoroughly shaken, in a cylinder, the suspension is set down and the sedimentation process is allowed to begin.

Interpretation of the sedimentation analysis is based on the Stokes law which expresses the terminal velocity (v) with which a spherical particle will fall through water as a function of the square of the particle diameter (D) in the form:

v= (Gs- Gw)ρw18η D2

where,		η = coefficient of dynamic viscosity of water = 9.12 x 10-6 gs/cm2

Gs= specific gravity of soil particles = 2.65

Gw= specific gravity of water = 1.00

ρw= density of water = 1.00 g/cm3

Thus,

v=100.51 D2

where, v  is in cm/s.

Thus, at a depth (L, cm) within the suspension after a time (t,sec), there will be no particles larger than

D= L100.51 t

All particles smaller than this value of D will be at a concentration unchanged from that at the start of sedimentation.  This concentration is a measure of the mass of particles in the original suspension having particle size finer than D. One procedure for determining the concentration is the pipette method in which a small specimen of the suspension is withdrawn from a depth L=10 cm at a specified time t.  The specimen is dried and the mass of solid residue obtained and used to determine the mass of particles in the original suspension having a diameter less than

D= 10100.51 t

The mass of particles finer than in the original sample is then obtained by simple proportion.  Repeating this procedure at various times after the start of sedimentation enables the particle size analysis to be completed and the grading curve for the soil extended through the silt range.

The grading curve: When the particle size analysis is complete, a grading curve is plotted in which the % mass by mass of particles finer than any particle size is plotted against the sizes of particles to a logarithmic scale.  The shape of the grading curve indicates whether a soil contains a wide range or only a limited range of particle sizes and this is used to formulate a description of the grading of the soil.  A coarse grain soil is described as well-graded if it contains approximately equal proportion of all particle sizes and is characterized by a relatively smooth curve covering a wide of particle sizes.  On the other hand, a coarse grain soil may be poorly graded if: a) a high proportion of the particles lie in a narrow size band.  In this case, the soil may be described as uniform; b) the soil contains large and small particles but exhibit an absence of particles in the intermediate size range.  This may be described as gap-graded.

An indication of the grading curve may be expressed numerically in terms of the coefficient of uniformity (Cu), and the coefficient of curvature (Cz) defined as:

Cu= D60D10

Cz= D302D60D10

where, D10, D30,   D60= particle size such that 10, 30 and 60 % respectively of the material finer than the size.

If Cu>4 or 1<Cz<3, then the soil is well graded, otherwise it is poorly graded.

Consistency of Clays and Atterberg Limits

One of the most important characteristics of clay soil is its plasticity.  The extent to which natural clay exhibits plasticity depends upon its clay mineral composition and water content.  The consistency of natural clay is found to change with water content from the solid dry state through the semi-solid or non-plastic state to plastic and liquid states as the water content increases.  These consistency states do vary from one type of clay to the other.  The change from one consistency state to another is gradual but for purposes of classification, arbitrary limits have been established to differentiate between the various consistency states.  These divisions or limits are referred to as Atterberg limits.  The Atterberg limits are the following:

- Shrinkage limit (Ws): the change from the solid to the semi-solid or non-plastic state.  This is the maximum water content at which further loss of water does not cause a decrease in the volume of the soil.  In the context of soil classification, the shrinkage limit is relatively unimportant.

- Plastic limit (Wp): the change from non-plastic to plastic state.  This is the minimum water content at which the soil can be rolled into a thread 3 mm diameter without breaking up.

- Liquid limit (Wl): the change from plastic to liquid state.  This is the minimum water content at which the soil will flow under its own weight.

It is important to note that Atterberg limits are simply water contents.  The range of water content over which clay exhibits plasticity is termed the plasticity index (Ip ):

Ip = Wl- Wp

The natural water content (W) at which clay exists in a field may be compared with its liquid and plastic limits by reference to the liquidity index (Il) which is defined as:

Il= W- WpWl- Wp= W- WpIp

If Il approaches 1.0, then the clay water content is said to be approaching its liquid limit.  If Il approaches zero, the clay water content is said to approaching its plastic limit.  For practical applications, 0≤Il≤1, but under field conditions, it is possible to have W≤ Wp, thus causing Il to be in the negative.

Plasticity is attributed to the deformation of the adsorbed water around clay mineral particles which is known as the activity of the clay, defined as:

A= Ip % clay

where, the % clay is taken as the percentage by mass finer than 0.002 mm.  Activity of clay is a measure of the degree of plasticity.  Generally, there 3 types of clays: kaolinite, illite and montmorillonite, with increasing activity in that order.

Determination of plastic and liquid limits:  Standard methods exist for the determination of plastic and liquid limits but these tests are carried out on remoulded soil in the laboratory and cannot therefore be expected to reflect characteristics of engineering behavior under natural undisturbed conditions in the field.

For plastic limit determination, about 20 g of dried soil, all passing the 0.425 mm sieve are mixed with distilled water and moulded into a ball.  The ball of soil should be rolled by hand on a glass with sufficient pressure to form a thread.  When the diameter of the resulting thread becomes 3 mm the soil is kneaded and then rolled out again.  The process is continued until the thread crumbles when it is 3 mm diameter. At this stage, the water content of the soil is determined.  The procedure should be carried out at least twice and the average value determined.

For liquid limit determination, a sample of oven-dried soil, all passing the 0.425 mm sieve, is mixed with distilled water to a stiff consistency, a portion of it is placed in the penetrometer cup, the soil being struck off level with the top of the cup.  The penetrometer cone is then clamped with its tip just touching the soil.  The clap is released, the cone allowed to penetrate the soil for 5 seconds, the clamp is reapplied and the amount of penetration read on the dial gauge.  This is repeated until two successive tests give the same readings.  At this stage, the water content of the soil in the cup is determined.  The whole procedure is repeated with successive additions of distilled water to the sample, and the relationship between water content and cone penetration plotted and fitted with the best straight line and the water content corresponding to 20 mm cone penetration read off as the liquid limit.

| Figure 1. Penetrometer test | Problems - The results of a sieve analysis of a soil were as follows: Sieve size (mm); 50; 37.5; 19; 12.5; 8; 5.9; 4.75; 2.8. Weight retained (g); 0; 15.5; 17; 10; 11; 33; 33.5; 81. Sieve size (µm); 2360; 1300; 400; 212; 150; 100; 75. Weight retained (g); 18; 31; 32.5; 9; 8; 5.5; 5. The total weight of the sample was 311g. Plot the particle size distribution curve and give a description of the soil. - A liquid limit test carried out on a sample of inorganic soil taken from below the water table gave the following results: Cone penetration (mm); 15.5; 18.2; 21.4; 23.6. Water content (% wt); 34.6; 40.8; 48.2; 53.4. A plastic limit test gave a value of 33 %. Determine the liquid limit and plasticity index of this soil. |
| --- | --- |