KWAME NKRUMAH UNIVERSITY OF SCIENCE AND TECHNOLOGY

COLLEGE OF ENGINEERING

DEPARTMENT OF AGRICULTURAL ENGINEERING

AE 352

SOIL MECHANICS LAB REPORT

GROUP 6

Bright Frimpong			4164515

George Marfo			4166015

Joel Ohene Frimpong		4164615

Priscilla Opoku Agyeiwaa 	4167015

Emmanuel Boakye Addo   	4161715

Samuel Mensah Dwamena	4164215

Bright Tenkorang Ofori 		4166715

Ambrocius Asiedu Addo		4163115

April 2018

ABSTRACT	3

PARTICLE SIZE DISTRIBUTION TEST	4

Introduction	4

Aim	4

Apparatus	4

Procedure	4

Tables and Results	5

CONCLUSION	7

LIQUID LIMT TEST	8

Introduction	8

Aim	8

Apparatus	8

Procedure	8

Tables and Results	9

Conclusion	10

PLASTIC LIMIT	11

Introduction	11

Aim	11

Apparatus	11

Procedure	11

Table and Results	12

Conclusion	12

Hydrometer Analysis	13

Introduction	13

Aim	13

Apparatus	13

Sample Preparation	13

Procedure	14

Table and Results	14

Conclusion	15

COMPACTION	16

Introduction	16

Aim	16

Apparatus	16

Procedure	16

Table and Results	17

Conclusion	18

SPECIFIC GRAVITY TEST	19

Introduction	19

Aim	19

Apparatus	19

Procedure	19

Table and Results	20

Conclusion	20

TRIAXIAL TEST	21

Introduction	21

Aim	21

Apparatus	21

Procedure	21

Table and Results	22

Precaution	23

Conclusion	23

Appendix	24

References	24

# ABSTRACT

This is a report based on seven (7) experiments performed at the geotechnical laboratory. The experiments are particle size distribution, hydrometer analysis, liquid limits, plastic limits, compaction, triaxial and specific gravity test. In each of experiments are the results obtained from the laboratory after each experiment, attached with their graphs and necessary calculations.

# PARTICLE SIZE DISTRIBUTION TEST

## Introduction

Particle size distribution refers to the proportions by dry mass of a soil distributed over specified particle-size ranges. Particle size distribution is used to classify soils for engineering and agricultural purposes, since particle size influences how fast or slow water or other fluid moves through a soil.

## Aim

The purpose of this experiment was to determine particles finer than coarser.

## Apparatus

Balance

Sieves

Sieve shaker

Oven

Trays

Sieve brush

Riffle box

## Procedure

- A sample of soil is obtained, the sample is poured into a riffle box. The sample is divided into two equal parts in each riffle box. The sample in one of the boxes is picked and weighed between 500-1000gm and recorded using the balance.

- The sample weighed is passed through a BS test sieve 2mm.

- The sample fraction greater than 2mm is poured into a rubber bowl flooded with water for 24hrs.

- The sample fraction smaller than 2mm is weighed between 50-100gm and recorded, the weighed sample is poured into a rubber bowl and flooded with water for 24hrs.

- Wash both soaked samples thus step 3 & 4 over a 2mm and 0.075mm sieve respectively and dried in the oven for at least 16hrs.

- The BS test sieve is selected and arranged in the order as follows (2.00, 3.18, 4.75, 6.70, 9.50, 13.20,19.00) mm for sample greater than 2mm and (0.075, 0.100, 0.200, 0.300, 0.425, 0.600, 1.00) mm.

- The sample is separated into various fractions by sieving through the selected sieves in descending order with the help of the sieve shaker (for about 10mins)

- The mass retained on each sieve is weighed and recorded.

## Tables and Results

For sample fraction greater than 2mm

Mass Of sample = 900gm

| Sieve Size (mm) | Weight of soil retained (g) | Cumulative weight of soil retained (g) | Cumulative weight of soil retained (%) | Percentage (%) finer than |
| --- | --- | --- | --- | --- |
| 19.00 | 9.86 | 9.68 | 1.08 | 98.92 |
| 13.20 | 16.36 | 26.04 | 2.89 | 97.11 |
| 9.50 | 53.59 | 79.63 | 8.85 | 91.15 |
| 6.70 | 96.97 | 176.60 | 19.65 | 80.38 |
| 4.75 | 128.99 | 305.59 | 33.95 | 66.05 |
| 3.18 | 108.11 | 413.70 | 45.97 | 54.03 |
| 2.00 | 70.79 | 484.49 | 53.83 | 46.17 |

For sample fraction less than 2mm

Mass of sample = 75gm

| Sieve Size (mm) | Weight of soil retained (g) | Cumulative weight of soil retained (g) | Cumulative weight of soil retained (%) | Percentage (%) finer than | Corrected (%) |
| --- | --- | --- | --- | --- | --- |
| 1.00 | 9.27 | 9.27 | 12.36 | 87.64 | 40.46 |
| 0.600 | 2.86 | 12.13 | 16.17 | 83.83 | 38.70 |
| 0.425 | 1.74 | 13.87 | 18.49 | 81.51 | 37.63 |
| 0.300 | 0.66 | 14.53 | 19.37 | 80.63 | 37.23 |
| 0.200 | 1.54 | 16.07 | 21.43 | 78.57 | 36.28 |
| 0.100 | 3.10 | 19.17 | 25.56 | 74.44 | 34.37 |
| 0.075 | 0.01 | 19.18 | 25.57 | 74.43 | 34.36 |

Correction factor = 0.4617

D60 = 4, D30 = 0 D10 = 0

## CONCLUSION

This experiment was performed to show how particle sizes are classified and this will help the engineer know the type of particle or material needed for a work or project. Since there was no 30% and 10% finer, the soil was not graded.

# LIQUID LIMT TEST

## Introduction

The change from plastic to liquid state. This is the minimum water content at which the soil will flow under its own weight.

## Aim

To determine the liquid limit of the soil.

## Apparatus

Balance

Casagrande

Grooving tools

Two spatulas

Two Handkerchief (wet & dry)

Flat board

Oven

Wash bottle

Container for moisture content

## Procedure

- The mass of five moisture containers are determined with the aid of a balance

- A sample is obtained and sieved through 0.425 sieve

- About 250gm of the sieved sample passing through 0.425mm sieve is weighed and poured on the flat board.

- The sample is mixed with distilled water to form uniform paste with consistency that would require 40 to 50 drops of cup to cause closer of groove to the length of 10mm.

- A portion of the paste to be placed in the cup of the Casagrande

- Spread it with few strokes of spatula of about 1cm into the Casagrande cup

- Divide the soil in the cup into two equal parts using a grooving tool

- Turn the crank of the Casagrande at two revolutions per second until the two halves of soil cake meet each other for the length of 10mm.

- The number of blows required to cause the groove close for about 10mm is recorded.

- A sample of the soil is taken, and its water content is determined.

- The sample left in the cup is added to the remaining sample on the flat board, the wet and dry handkerchiefs is used to clean and dry the cup of the device.

- The process is repeated with different moisture contents for at least four more times for the blows between 10 and 50.

## Tables and Results

Liquid Limits table

| Container No | gm | K3 | A10 | C7 | A6 | C9 |
| --- | --- | --- | --- | --- | --- | --- |
| Mass of container | gm | 3.69 | 3.82 | 3.69 | 3.61 | 3.75 |
| Number of blows | gm | 46 | 36 | 27 | 15 | 6 |
| Mass of container & wet sample | gm | 10.38 | 12.49 | 10.60 | 10.16 | 12.86 |
| Mass of container & dry sample | gm | 8.38 | 10.09 | 8.66 | 8.16 | 9.91 |
| Mass of water | gm | 2 | 2.4 | 1.94 | 2 | 2.95 |
| Mass of dry sample | gm | 4.69 | 6.27 | 4.97 | 4.55 | 6.16 |
| Water Content | % | 42.64 | 38.28 | 39.03 | 43.96 | 47.89 |

At the 25 blows, water content is 42.2%

Liquid limit = 42.2%

## Conclusion

The liquid limit of the soil sample was determined.

# PLASTIC LIMIT

## Introduction

The change from non-plastic to plastic state. This is the minimum water content at which the soil can be rolled into a thread 3 mm diameter without breaking up.

## Aim

To determine the moisture content of soil.

## Apparatus

Balance

Container for moisture content

Two spatulas

Flat board

Oven

Wash bottle containing distilled water

## Procedure

- The sample is sieved through 0.425mm BS sieve.

- About 30gms of sieved sample is taken and mixed with distilled water on a flat board to form a uniform paste with consistency.

- Take about 10gms of the plastic soil mass and roll it between fingers on a flat board.

- The sample is rolled into a thin thread of about 3mm diameter through the length

- When the sample begins to disintegrate, the pieces are collected into a container and dried in an oven for at least 16hrs.

- Record the dry weight of the sample after 16hrs

- Repeat the test for the remaining half

## Table and Results

| Container Number | gm | B6 | C35 |
| --- | --- | --- | --- |
| Mass of container | gm | 3.41 | 3.78 |
| Mass of container &Wet sample | gm | 6.33 | 7.02 |
| Mass of container & dry sample | gm | 5.95 | 6.53 |
| Mass of Water | gm | 0.38 | 0.49 |
| Mass of dry sample | gm | 2.54 | 2.75 |
| Water content | % | 14.96 | 17.82 |
| Average Water content | % | 16.39 |  |

Plastic limit = 16.39%

Ip=Wl- Wp

Ip=42.2-16.39=25.81%

## Conclusion

The plastic limit of the soil sample is determined and since the liquid limit is not greater than 50%, plasticity is low.

# Hydrometer Analysis

## Introduction

Hydrometer analysis is primarily used to know the grain size distribution of a fine-grained soil. This is because a fine-grained soil consists of different sizes of particles starting from 0.075 mm to 0.0002 mm and it is not practicable to design sieve having so smaller screen size. Therefore, hydrometer analysis is done for grain size analysis of fine grained soils. Hydrometer analysis is based on Stokes law. It states that “the velocity at which grains settles out of suspension, all other factors being equal, is dependent upon the shape, weight and size of the grain”.

## Aim

To determine the grains, settle out suspension of fine grained soils.

## Apparatus

Hydrometer

Two glass measuring cylinder (1000ml&100ml)

Thermometer

Stirring apparatus

BS Sieve (0.075mm or 75 microns)

Stop watch

Wash bottle containing distilled water

Glass rod

Dispersion agent (33gm of sodium hexametaphosphate and 7gms of sodium carbonate dissolve in 1000ml of distilled water)

## Sample Preparation

- The sample obtained is sieved through 75 microns BS sieve and weighed between 15-25gms.

- The sample is poured into the cup, with the aid of a stirring rod 100ml sodium hexametaphosphate and distilled water is added and stirred for at least 15mins

- The mixed solution is poured into the 1000ml glass measuring cylinder and left-over night.

## Procedure

- The solution is remixed thoroughly while putting your palm (stopper) on the mouth of glass measuring cylinder

- After mixing the soil solution thoroughly, place the content on level surface.

- With the aid of a stopwatch take the hydrometer readings corresponding to the upper meniscus at an interval of 30sec,1minute, 2minutes.

- After taking the 2minutes reading remove the hydrometer from the solution.

- For each reading take the temperature of the solution

- Continue the reading by inserting the hydrometer into the solution for the following time intervals (4,8,15,30,60,120,240,1440) minutes.

## Table and Results

| Elapsed time (min) | Temp (℃) | Direct hydrometer readings(Rh’) | Reading Rh’ | Rh=Rh’+cm | Hr (mm) | Viscosity | D (mm) | Temp corr,Mt | Rd=Rh’-Ro+Mt | K (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.50 | 25 | 1.0112 | 11.2 | 11.7 | 156.36 | 0.89 | 0.0716 | 1.03 | 8.97 | 71.87 |
| 1.00 | 25 | 1.0102 | 10.2 | 10.7 | 160.31 | 0.89 | 0.0513 | 1.03 | 7.97 | 63.86 |
| 2.00 | 25 | 1.0095 | 9.5 | 10 | 161.1 | 0.89 | 0.0363 | 1.03 | 7.27 | 58.25 |
| 4.00 | 25 | 1.0085 | 8.5 | 9 | 165.05 | 0.89 | 0.0260 | 1.03 | 6.27 | 50.24 |
| 8.00 | 23 | 1.0083 | 8.3 | 8.8 | 165.84 | 0.93 | 0.0188 | 0.59 | 5.63 | 48.63 |
| 15.00 | 23 | 1.0080 | 8 | 8.5 | 167.03 | 0.93 | 0.0138 | 0.59 | 5.33 | 46.23 |
| 30.00 | 23 | 1.0078 | 7.8 | 8.3 | 167.82 | 0.93 | 0.00979 | 0.59 | 5.13 | 44.63 |
| 60.00 | 23 | 1.0076 | 7.6 | 8.1 | 168.61 | 0.93 | 0.00694 | 0.59 | 4.93 | 43.02 |
| 120.00 | 24 | 1.0073 | 7.3 | 7.8 | 169.79 | 0.91 | 0.00487 | 0.81 | 4.85 | 40.62 |
| 240.00 | 23.5 | 1.0071 | 7.1 | 7.6 | 170.58 | 0.92 | 0.00347 | 0.69 | 4.53 | 39.02 |
| 1440.00 | 25 | 1.0061 | 6.1 | 6.66 | 174.53 | 0.89 | 0.00141 | 1.03 | 3.87 | 31.01 |

D60 = 0.04mm

## Conclusion

The grain sizes during settle out of suspension was achieved and since there was no 30% and 10% finer the soil could not be graded.

# COMPACTION

## Introduction

Compaction is the term used to describe the process where, by mechanical means, increase in soil density is achieved by decreasing the air voids content with the water content remaining approximately the same. Compaction increases the shear strength and thereby improving the stability of embankments and the bearing capacity of foundations and pavements, decreasing compressibility and thereby reducing settlements, decreasing the void ratio and thereby reducing the soil permeability, by reducing the potential for swelling and shrinkage.

## Aim

To determine optimum moisture content and the maximum dry density

## Apparatus

Cylindrical metal mould, base plate collar and metal block

A standard hammer of weight 4.5kg

Balance for weighing

Oven

Containers for moisture content

## Procedure

- Sieve the material provided through BS test sieve 19mm.

- Weigh 700 of the sieved material.

- Weigh the mould and base plate.

- Find the volume of the mould with the metal block in it.

- Mix weighed sample with water at a percentage of ranging from 2% to 5% depending upon fines within the material at hand.

- Fill the mold in 5 layers, compact each layer by 55 blows with hammer, the compacted sample must be above the height of the mould.

- Trim the soil to the height of mould and weigh mould with soil.

- Take two containers and filled them half way the soil sample and determine the moisture content.

- Repeat the process from step 5 until the mass of the mould and soil start to fail.

## Table and Results

| Mass of cylinder + wet sample (gm) | 11766 | 12229 | 12337 | 12139 | 11982 |
| --- | --- | --- | --- | --- | --- |
| Mass of cylinder (gm) | 7177 | 7177 | 7177 | 7177 | 7177 |
| Mass of wet sample (gm) | 4589 | 5052 | 5160 | 4962 | 4805 |
| Bulk Density (gm/cc) | 2.133 | 2.349 | 2.399 | 2.307 | 2.234 |

| Container no. | 9z | S4 | S6 | GK2 | NE1 | XXV | PB4 | S26 | A40 | E2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mass of container + wet soil (gm) | 141.98 | 99.42 | 107.15 | 100.43 | 91.54 | 91.57 | 102.27 | 109.63 | 118.93 | 116.39 |
| Mass of container + dry soil (gm) | 136.91 | 94.79 | 100.80 | 95.05 | 86.62 | 83.83 | 94.52 | 101.57 | 109.53 | 105.94 |
| Mass of container (gm) | 25.50 | 13.75 | 13.69 | 14.42 | 13.80 | 13.49 | 13.48 | 15.69 | 14.75 | 14.80 |
| Mass of wet soil (gm) | 116.49 | 85.67 | 92.73 | 86.74 | 77.74 | 78.08 | 88.79 | 93.94 | 104.18 | 101.59 |
| Mass of dry soil (gm) | 111.41 | 81.04 | 86.38 | 81.36 | 72.82 | 70.34 | 81.04 | 85.88 | 94.78 | 91.14 |
| Mass of water (gm) | 5.08 | 4.6 | 6.35 | 4.38 | 4.92 | 7.74 | 7.75 | 8.06 | 9.40 | 10.45 |
| Water Content (%) | 4.56 | 5.68 | 7.35 | 5.38 | 6.76 | 11 | 9.56 | 9.39 | 9.92 | 11.47 |
| Average water content (%) | 5.12 |  | 6.37 |  | 8.88 |  | 9.48 |  | 10.70 |  |
| Dry density (gm/cc) | 2.029 |  | 2.208 |  | 2.203 |  | 2.107 |  | 2.018 |  |

Height of mould = 11.7cm

Diameter of mould = 15.3cm

Volume of mould = π(15.3)24×11.7=2151.090cm3

Maximum dry bulk density = 2.31 gm/cc

Optimum water content = 7.6%

## Conclusion

The maximum dry bulk density and optimum water content values for the soil sample was determined.

# SPECIFIC GRAVITY TEST

## Introduction

Specific gravity is the ratio of the weight in air of a given volume
of a material at a standard temperature to the weight in air of an equal volume of distilled water at the same stated temperature.

## Aim

To determine specific gravity of fine-grained soil by density bottle method.

## Apparatus

Balance

Glass Jar

Dry cloth

Shallow Tray

Glass Lid

Rubber stopper

Wash bottle containing distilled water

## Procedure

- Pour soil sample into the bottle about half

- Record mass of soil in glass vessel plus glass lid

- Add water to the sample to be little above the height of the soil sample

- Fix rubber stopper in the glass vessel and agitate sample to remove entrapped air (clockwise and anti-clockwise rotation of the glass vessel).

- After shaking place, the glass vessel on level surface without any disturbance for 16hrs

- After 16hrs carefully place the glass vessel in a shadow bowl or tray.

- Top up the water to the brim and carefully slide the glass lid without trapping air.

- Clean bottle leaving no evidence of water, weigh and record mass of the bottle and content plus lid.

- Pour sample out of bottle then clean the bottle, weigh and record mass of the bottle with water only plus glass lid.

## Table and Results

| Mass of empty glass jar + lid (g) | 412 |
| --- | --- |
| Mass of glass jar + Agg + lid (g) | 1018 |
| Mass of glass jar + Agg+ water + lid (g) | 1754 |
| Mass of glass jar + water + lid (g) | 1376 |
| Mass of Aggregate (g) | 606 |
| Mass of water (g) | 964 |
| Mass of water used (g) | 736 |
| Volume of Aggregate (g) | 228 |
| Specific Gravity | 2.66 |

Volume of aggregate = mass of water – mass of water used

=	964 – 736 = 288g

Specific gravity =Mass of Aggregatevolume of Aggregate

= 606228=2.66

## Conclusion

The specific gravity of a fine grain soil was attained after the experiment was performed.

# TRIAXIAL TEST

## Introduction

A triaxial shear test is a common method to measure the mechanical properties of many deformable solids, especially soil (e.g., sand, clay) and rock, and other granular materials or powders.

## Aim

To determine the shear strength of the soil

## Apparatus

A 3.8 cm (1.5 inch) internal diameter long sample tubes.

Rubber ring.

Moisture content test apparatus

Balance

## Procedure

- The sample is setup, water is admitted, and the cell is fitted under water escapes from the bed valve, at the top, which is closed. Testing the sample at zero lateral pressure water is not required.

- The air pressure in reservoir is then increased to raise the hydrostatic pressure in the required amount. The pressure gauge must be watched during the test and any necessary adjustment must be made to keep the pressure constant.

- The handle wheel of the screw jack is rotated until the underside of the hemisphere seating of the proving ring, through which the loading is applied, just touches the cell piston.

- The piston is then removed down by handle until it is just in touch with the pressure plate on the top of the sample, and the pivoting ring seating is again brought into contact for the begging of the test.

- The machine is set in motion (or if hand wheel is turned at a constant rate) to give a rate of strain 2% per minute. The strain dial gauge reading is recorded to the corresponding proving ring reading is taken from the corresponding proving ring chart.

- The load applied is known. The experiment is stopped at the strain dial gauge reading for 15% length of the sample.

## Table and Results

| Change in length (div) | Strain (%) | New Area (mm2) | Proving ring Reading (div) | Deviator stress (kPa) | Proving ring reading (div) | Deviator stress (kPa) | Proving ring reading (div) | Deviator stress (kPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.00 | 1134.26 | 0 | 0 | 0 | 0 | 0 | 0 |
| 10 | 0.25 | 1138.06 | 1 | 7.2 | 7.5 | 53.8 | 9.6 | 68.8 |
| 20 | 0.51 | 1141.87 | 2 | 14 | 11 | 78.6 | 12 | 85.8 |
| 30 | 0.76 | 1145.72 | 5 | 36 | 13 | 92.6 | 16 | 113.9 |
| 40 | 1.02 | 1149.59 | 8 | 56.8 | 17 | 120.7 | 18.1 | 128.5 |
| 50 | 1.27 | 1153.49 | 9.5 | 67.2 | 19 | 134.4 | 21 | 148.6 |
| 60 | 1.52 | 1157.41 | 11 | 77.6 | 21 | 148.1 | 24 | 169.2 |
| 70 | 1.78 | 1161.36 | 12.5 | 87.8 | 23 | 161.6 | 24.5 | 172.1 |
| 80 | 2.03 | 1165.34 | 13.5 | 94.5 | 25 | 175.7 | 26.5 | 185.6 |
| 90 | 2.29 | 1169.34 | 15 | 104.7 | 27 | 188.4 | 28 | 195.4 |
| 100 | 2.54 | 1173.37 | 15.5 | 107.8 | 29 | 201.7 | 29 | 201.7 |
| 120 | 3.05 | 1181.52 | 17.5 | 120.9 | 33 | 227.9 | 32.5 | 224.5 |
| 140 | 3.56 | 1189.79 | 19.5 | 133.7 | 36 | 246.9 | 35 | 240 |
| 160 | 4.06 | 1198.79 | 20.8 | 141.6 | 39 | 265.5 | 36.5 | 248.5 |
| 180 | 4.57 | 1206.66 | 22.5 | 152.2 | 42 | 284 | 38.5 | 260.4 |
| 200 | 5.08 | 1215.28 | 23.8 | 159.8 | 43.5 | 292.1 | 40.5 | 271.9 |
| 250 | 6.35 | 1237.38 | 26.5 | 174.8 | 47.5 | 313.2 | 44 | 290.2 |
| 300 | 7.62 | 1260.29 | 29.5 | 191.0 | 51.5 | 333.4 | 47.5 | 307.5 |
| 350 | 8.89 | 1284.07 | 32 | 203.4 | 54.5 | 346.3 | 50 | 326.9 |
| 400 | 10.16 | 1308.76 | 34.5 | 215.1 | 57 | 355.4 | 53 | 330.5 |
| 450 | 11.43 | 1334.43 | 36 | 220.1 | 59 | 360.8 | 55 | 336.3 |
| 500 | 12.70 | 1361.11 | 37.5 | 224.8 | 61 | 365.7 | 57 | 341.7 |
| 550 | 13.97 | 1388.89 | 39 | 229.1 | 62 | 364.3 | 59 | 346.6 |
| 600 | 15.24 | 1417.83 | 40.5 | 233.1 | 64 | 368.3 | 60.5 | 348.2 |
| 700 | 17.78 | 1479.47 | 42 | 231.7 | 66 | 364 | 63.9 | 352.4 |
| 800 | 20.32 | 1546.72 | 43 | 226.9 | 67 | 353.5 | 66 | 348.2 |
| 900 | 22.86 | 1620.37 | 43.5 | 219.1 | 68 | 342.4 | 68.2 | 343.4 |

| Test | Cell pressure σ3/kPa | Deviator stress (kPa) | Major Principal stress σ1/kPa | Centre kPa | Radius kPa |
| --- | --- | --- | --- | --- | --- |
| 1 | 100 | 231 | 331 | 215.5 | 115 |
| 2 | 200 | 331 | 531 | 365.5 | 165 |
| 3 | 300 | 370 | 670 | 485 | 185 |

τ=c+ σ tanφ

τ= 59 + 670 tan (11) = 189.23 kN/m2

## Precaution

- Prevent any part of the machine or cell from jogging the sample while setting up.

- Cell must be properly set up and clamped to prevent leakage of pressure during the test.

## Conclusion

The shear strength of the soil was obtained at the end of the experiment with a graph showing peak of the various deviator stress thus the principal minor stress.

# Appendix

Casagrande device                                Hydrometer                         Triaxial device

# References

Prof. S.K. Agodzo, KNUST, soil mechanics application to mechanization.

William Powrie, soil mechanics concept and applications, 2nd edition.

Www.theconstructor.org/geotechnical