# KWAME NRUMAH UNVERSITY OF SCIENCE & TECHNOLOGY

COLLEGE OF ENGINEERING

DEPARTMENT OF AGRICULTURAL & BIOSYSTEMS ENGINEERING

SOIL MECHANICS LAB REPORT

GROUP 10

MAY 7, 2019

GROUP MEMBERS

- Broni Anita                           6027016

- Adamtey Eugene                  6023216

- Wiafe Evans Kofi                  6033816

- Aidoo Samuel Philips            6024416

- Appiah Kevin Ofosuhene      6025316

- Amo Parker Prince               6024616

- Gyamfi Opoku Caleb            6028716

- Asafo Agyei Emile                6025616

- Nii Adotey Addo                   6023416

GENERAL INTRODUCTION

In engineering, the soil considered as a loose sedimentary material such as clay, silt, sand or gravel or a mixture of these materials. All engineering structures like building, bridge, highway, tunnel, dam, tower, etc are founded below or on the surface of the earth. The subsoil is of greater interest in the construction of these structures because it harbours the entire weight of the soil to be able to hold the structures. This is the more reason why the topsoil is removed prior to construction works, since it is weak in weight due to the presence of organic matter which decomposes with respect to time and changes the behaviour of the soil.

To check the suitability of the soil to be used as foundation or as construction materials, its properties are required to be assessed. Geotechnical engineering is a discipline of engineering that deals with the study of the soil and bedrocks, especially aspects of foundations and earthworks. Soil mechanics is a branch in geotechnical engineering that deals with soil behaviour.

Atterberg Limit test, Particle sizes distribution test, Hydrometer analysis, Specific gravity test, Compaction test and Triaxial test were conducted in this study. All these tests are needed to generate the relevant input data for the design and construction of foundations for proposed structures.

Experiment 1: Atterberg Limit Test

LIQUID AND PLASTIC LIMIT TEST

Introduction

Atterberg limits or liquid and plastic limits are simply water contents of a soil sample. The liquid limit of a soil sample is the water content at which the soil will flow under its own weight. It is from this principle that landslides are created or formed.

Plastic limit is the transition between semi-solid and plastic state. These are water contents at which a soil sample can be rolled into threads of 3 mm without breaking.

Apparatus

- Balance

- Liquid limit device (Casagrande Apparatus)

- Grooving tools

- Two Spatula

- Two handkerchief (wet and dry)

- Flat board

- Oven

- Wash bottle containing distilled water

- Container for moisture content

- Mortar and pestle

LIQUID LIMIT TEST

Procedure

- The mass of each of the five moisture containers provided was determined.

- The soil sample collected was sieved through a sieve size of 0.425mm.

- About 300g of the sieved sample passing through the 0.425mm sieve was weighed and poured onto a flat board.

- The sample on the flat board was then mixed with the distilled water to form a uniform paste with consistency requiring 40 to 50 drop of cup to cause closer groove to a length of 10mm.

- A portion of the paste was placed in the cup of the liquid limit device (Casagrande Apparatus).

- The paste (soil) was spread with few strokes of spatula.

- The paste was trimmed to a depth of 1cm at the point of maximum thickness and the excess of the soil was placed returned to the flat board.

- The soil in the cup was divided by a firm stroke of the grooving tool along the diameter through the center line of the cup.

- The cup was lifted and dropped by turning the crank at a rate of 2rps until the two halves of the cake came into contact with each other for the length of about 10mm.

- The number of blow required to cause the groove to close was recorded.

- A sample of the soil was taken and its water content was determined.

- The soil left in the cup was added to the remaining soil on the flat board and the cup cleaned.

- The whole process was repeated from step 2 with four different moisture containers for the blows between 10 and 50.

- The corresponding water content at (100±5°C) for at least 16 hours was determined and a “flow curve” of number of blows verses water content (%) was plotted

Casagrande Apparatus

Results & Discussion

Table of values for the Liquid Limit Test

| Container No. | g | C26 | B21 | A31 | B16 | A7 |
| --- | --- | --- | --- | --- | --- | --- |
| Mass of Container | g | 3.81 | 3.83 | 3.78 | 3.82 | 3.79 |
| No of blows | g | 9 | 14 | 25 | 38 | 47 |
| Mass of Container & Wet Sample | g | 12.50 | 13.37 | 15.75 | 17.04 | 19.18 |
| Mass of Container & Dry Sample | g | 11.04 | 11.93 | 13.64 | 14.44 | 15.92 |
| Mass of Water | g | 1.46 | 1.44 | 2.11 | 2.60 | 3.26 |
| Mass of Dry Sample | g | 7.23 | 8.10 | 9.86 | 10.62 | 12.13 |
| Water content | % | 20.19 | 17.83 | 21.40 | 24.48 | 26.88 |

Graph of No. of Blows Verses Water Content

From the graph, the liquid limit, WL=20.8%

PLASTIC LIMIT TEST

Procedure

- The mass of each of the two moisture containers provided was determined.

- The soil sample was sieved using a 0.425mm sieve.

- 50g of the sieved sample was taken and thoroughly mixed with the distilled water on the flat board to form a uniform paste with consistency (the sample was mixed thoroughly with distilled water on the flat board until the soil mass became plastic to be easily molded with the fingers.)

- The paste was allowed to be seasoned for sufficient time, allowing water to permeate throughout the soil mass.

- About 10g of this plastic soil mass was taken and rolled between fingers and the flat board with just sufficient pressure rolling the mass into threads of 3mm diameter throughout its length.

- The soil mass was kneaded together forming a uniform mass and re-rolled.

- This process went on until the thread crumbled while the diameter was 3mm.

- Pieces of the crumbled thread was collected into a container for moisture content determination at (100±5°C) for at least 16 hours.

- The test was repeated for the remaining half.

- The average of the results calculated was taken to the nearest whole number.

Results & Discussion

Table of values for the Plastic Limit Test

| Container No | g | A2 | A25 |
| --- | --- | --- | --- |
| Mass of Container | g | 3.82 | 3.81 |
| Mass of Container & Wet Sample | g | 12.84 | 14.54 |
| Mass of Container & Dry Sample | g | 9.74 | 10.72 |
| Mass of Water | g | 3.10 | 3.82 |
| Mass of Dry Sample | g | 5.92 | 6.91 |
| Water Content | % | 52.36 | 55.28 |
| Average Water Content | % | 53.82 |  |

WP1=Mass of container & Wet sample-Mass of container & Dry sampleMass of Container & Dry sample-Mass of container×100

Wp1=12.84-9.749.74-3.82100=52.36%

WP2=Mass of container & Wet sample-Mass of container & Dry sampleMass of Container & Dry sample-Mass of container×100

Wp2=14.54-10.7210.72-3.81100=55.28%

Average WP = Plastic Limit = 53.82%

Plasticity Index IP = WL – WP

= (20.8 - 53.82) %

= - 33.02%

Conclusion

The tests were carried out on re-moulded soil sample in the laboratory and therefore, cannot be expected to reflect characteristics of engineering behaviour under natural undisturbed conditions in the field. Hence the results from both the plastic and liquid limit tests comes with an appreciable error with respect to the properties of the soil sample under engineering behaviour.

Experiment 2: PARTICLE SIZES DISTRIBUTION (PSD)

Introduction

Particle sizes distribution is vital in the classification and description of engineering soils. The sieve analysis grades sand and gravel while the sedimentation analysis grades the fraction of silt soil particles. This is expressed in terms of a grading curve or a particle size distribution curve in which the percentage by mass of particles finer than any particle size is plotted against particle size to a logarithmic scale.

Knowledge from the Particle sizes distribution of a soil sample provides basis of grouping soils according to their physical characteristics and appearance for the purposes of comparing different soil types. Soil engineering properties such permeability, strength, expansivity, etc may also be known from Particle Sizes Distribution Test.

Apparatus

- Balance

- Sieves

- Sieve shaker

- Oven

- Trays

- Sieve brush

- Riffle box

Sample preparation for wet sieving

- The soil sample provided was passed through a riffle box and (500 – 1000) g of it weighed.

- The weighed sample was sieved using BS test sieve 2.00mm.

- The fraction greater than 2.00 mm was poured into a rubber bowl and flooded with water for 24 hours.

- 50 – 100 g of the fraction smaller than the 2.00mm was weighed, poured into a rubber bowl and flooded with water for 24 hours.

- Both soaked samples in step 3 and 4 were washed over the 2.00mm and 0.15mm sieve respectively and dried in the oven for at least 16 hours.

Procedure

- The BS test sieve was selected and arranged in the order (2.00, 4.75, 6.70, 9.50, 13.20, 19.00, 37.50) mm for the sample greater than 2.00mm and (0.15, 0.200, 0.300, 0.425, 0.600, 1.00) mm for the sample smaller than 2.00mm.

- The sample was then separated into various fractions by sieving it through the above sieve in descending order by the application of the sieve shaker.

- The weight of soil retained on each sieve was recorded.

Result & Discussion

| Table of values for the sample greater than 2.00mm |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Sieve size(mm) | Weight retained(g) | Cumulative weight retained(g) | % Cumulative weight retained(g) | % Finer than | Log of sieve size |
| 37.50 | 0.00 | 0.00 | 0.00 | 100.00 | 1.57 |
| 19.00 | 18.21 | 18.21 | 5.17 | 94.83 | 1.28 |
| 13.20 | 48.40 | 66.61 | 18.92 | 81.08 | 1.12 |
| 9.50 | 43.05 | 109.66 | 31.15 | 68.85 | 0.98 |
| 6.70 | 39.16 | 148.82 | 42.27 | 57.73 | 0.83 |
| 4.75 | 56.58 | 205.40 | 58.34 | 41.66 | 0.68 |
| 2.00 | 146.67 | 352.07 | 100.00 | 0.00 | 0.30 |
| Table of values for the sample smaller than 2.00mm |  |  |  |  |  |
| 1.00 | 8.12 | 8.12 | 28.35 | 71.65 | 0.00 |
| 0.600 | 6.73 | 14.85 | 51.85 | 48.15 | -0.22 |
| 0.425 | 4.45 | 19.30 | 67.39 | 32.61 | -0.37 |
| 0.300 | 4.32 | 23.62 | 82.47 | 17.53 | -0.52 |
| 0.200 | 3.67 | 27.29 | 95.29 | 4.71 | -0.70 |
| 0.150 | 1.35 | 28.64 | 100.00 | 0.00 | -0.82 |

Grading curve for the soil sample greater than 2.00mm

From the grading curve,

D60=7,

D10=3 and

D30=4

Coefficient of uniformity, Cu=D60D10 =2.33

Coefficient of curvature, Cz=D302D10D60=0.762

Grading curve for the soil sample smaller than 2.00mm

From the grading curve,

D60=0.8,

D10=0.24 and

D30=0.4

Coefficient of uniformity, CU=D60D10 =3.33

Coefficient of curvature, CZ=D302D10D60=0.833

Conclusion

For well-graded soils, CU>4 and 1<CZ<3, otherwise poorly graded. From the results obtained from the grading curves above, it can be stated with certainty that the soil sample is poorly graded.

Experiment 3: SPECIFIC GRAVITY TEST

Introduction

Specific Gravity of a soil is the ratio of the mass of the soil solids to the mass of an equal volume of water. This property is needed since it reflects the history of weathering. It is also useful in soil mineral classification, for example iron minerals have larger value of specific gravity than silica. A knowledge on the specific gravity of a soil may also help in the calculation of other soil parameters such as void ratio, porosity, degree of saturation, etc.

In effect, the higher the value of the specific gravity, the higher the strength of the soil for engineering purposes such as road construction and foundation.

Apparatus

- Balance

- Glass Jar or shito bottle

- Dry Cloth

- Shallow Tray

- Glass Lid

- Rubber Stopper

- Wash bottle containing distilled water

Procedure

- The mass of the dry, empty clean bottle plus glass lid was determined (W1).

- The soil sample was poured into the bottle about halfway.

- The mass of the soil in the vessel plus glass lid was recorded (W2).

- Water was then added to the soil sample to a height a little above the soil sample.

- The rubber stopper was fixed in the glass vessel and the sample agitated to remove entrapped air. (This was achieved by rapid clockwise and anticlockwise rotation of the glass vessel between the hands.)

- The glass vessel was placed on a level surface without any disturbances for 16 hours after shaking.

- The glass vessel was then carefully placed in a shallow bowl or tray after the 16 hours.

- Water was added to the brim and then the glass lid carefully placed without trapping air.

- The bottle was cleaned leaving no evidence of water. The mass of the bottle and content plus lid was then recorded W3.

- The bottle was cleaned after the whole sample had been poured out. The bottle was filled with water to the brim and the mass of the bottle and content plus glass lid recorded W4.

Results and Discussion

Table of values

| Bottle No. | G10 |
| --- | --- |
| Mass of empty glass jar + lid W1 | 398.23 g |
| Mass of glass jar + Agg + lid W2 | 1003.53 g |
| Mass of glass jar + Agg + water + lid W3 | 1725.56 g |
| Mass of glass jar + water + lid W4 | 1367.11 g |
| Mass of Aggregate | 605.30 g |
| Mass of water | 968.88 g |
| Mass of water used | 722.03 g |
| Volume of Aggregate | 246.85 cm3 |
| Specific Gravity | 2.45 |

Volume of Aggregate = Mass of water – Mass of water used = 968.88 – 722.03 = 246.85 cm3

Specific Gravity of the soil =  Mass of soil solidsMass of an equal volume of water

= W2-W1W4-W1-W3-W2

= 1003.53-398.231367.11-398.23-(1725.56-1003.53)

SG = 2.45

Conclusion

Experimentally soil particles have their specific gravity between the range 2.65-2.85. Soil containing organic matter and porous particles may have their specific gravity below 2.0 and those with heavy substances above 3.0. It can then be concluded that a soil with Specific gravity of 2.45 is free from organic matter and porous particles.

Experiment 4: HYDROMETER ANALYSIS

Introduction

Hydrometer method is used to determine the particle size distribution of fine-grained soils including clay and silt particles. The hydrometer measures the specific gravity of the soil suspension at the center of its bulb. The specific gravity depends on the mass of solids present, which in turn depends on the particle size.

Apparatus

- Hydrometer

- Two glass measuring cylinder 1000ml and 100ml

- Thermometer

- Stirring apparatus

- Sieve 0.10mm or 100 micron

- Stop watch

- Wash bottle containing distilled water

- Glass rod

- Dispersion agent prepared from 33g of sodium hexametaphosphate and 7g of sodium carbonate dissolved in 1000ml of distilled water.

Theory

The procedure utilizes Stoke’s Law of settling velocity for spherical particles in a fluid;

V=29g(ρs-ρf)ηD22  , where;

η=Viscosity of water

ρs=Density of solids

ρf=Density of fluid(water)

g=acceleration due to gravity

D=Particle diameter

Solving this equation for D yields;

D=18ηVg(ρs-ρf)

To solve equation 2, the settling velocity, particle and fluid densities, and fluid viscosity must be known. A hydrometer is used to measure settling velocity and the remaining variables can be measured or estimated.

The settling velocity, V=Hrt , where;

Hr=distance particles fall in time t

t=time interval

From experiments, Hr can be determined by using

Hr=16.3-0.164Rh , where Rh’ = meniscus-corrected hydrometer reading

The percentage finer than the size D is given by : K%=ρsρs-1RdMs×100

Where; MS = Mass of dry soil used

Rd = Corrected hydrometer reading

Sample Preparation

- The sample provided was sieved through 0.1mm or 100 micron BS sieve and about (15-25) g weighed.

- The soil was poured into the cup of stirring apparatus and 100ml Sodium hexametaphosphate solution added. Some distilled water was added and then stirred for at least 15mins.

- The mixed solution was then poured into 1000ml glass measuring cylinder and left over night.

- The soil was remixed thoroughly while the palm was placed on the mouth of the glass measuring cylinder.

- The soil solution was placed on a level surface after a thorough mixing.

- Hydrometer readings corresponding to the upper meniscus was taken at an interval of 30sec, 1 minute, 2 minutes

- The hydrometer was removed from the solution after taking the 2 minutes reading.

- The hydrometer readings of the solution were taken for the following time interval from the start (4,8,15,30,60,120,240,1440) minutes.

- Hydrometer was not kept continuously in the solution.

Results and Discussion

Table of results

| Elapsed time(min) | Temp.(°C) | Direct Hydrometer readings Rh’ | Reading Rh’ | Rh=Rh’+Cm | Hr (mm) | η | D(mm) | Temp Corr. Mt | Rd=Rh’-Ro+Mt | K(%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.50 | 26 | 1.0140 | 14.0 | 16.0 | 161.333 | 0.874 | 0.0770 | 1.65 | 13.96 | 97.43 |
| 1.00 | 26 | 1.0280 | 13.0 | 15.0 | 161.335 | 0.874 | 0.0545 | 1.65 | 12.96 | 90.45 |
| 2.00 | 26 | 1.0120 | 12.0 | 14.0 | 161.337 | 0.874 | 0.0385 | 1.65 | 11.96 | 83.47 |
| 4.00 | 26 | 1.0100 | 10.0 | 12.0 | 161.340 | 0.874 | 0.0272 | 1.65 | 9.96 | 69.51 |
| 8.00 | 26 | 1.0100 | 10.0 | 12.0 | 161.340 | 0.874 | 0.0193 | 1.65 | 9.96 | 69.51 |
| 15.00 | 26 | 1.0095 | 9.5 | 11.5 | 161.341 | 0.874 | 0.0141 | 1.65 | 9.46 | 66.02 |
| 30.00 | 26 | 1.0090 | 9.0 | 11.0 | 161.342 | 0.874 | 0.0099 | 1.65 | 8.96 | 62.53 |
| 60.00 | 26 | 1.0090 | 9.0 | 11.0 | 161.342 | 0.874 | 0.0070 | 1.65 | 8.96 | 62.53 |
| 120.00 | 26 | 1.0085 | 8.5 | 10.5 | 161.343 | 0.874 | 0.0050 | 1.65 | 8.46 | 59.04 |
| 240.00 | 26 | 1.0075 | 7.5 | 9.5 | 161.344 | 0.874 | 0.0035 | 1.65 | 7.46 | 52.06 |
| 1440.00 | 26 | 1.0074 | 7.4 | 9.4 | 161.345 | 0.874 | 0.0014 | 1.65 | 7.36 | 51.37 |

Calculations

From standard tables from Bowles, J.E.1992, Engineering Properties of Soils and Their Measurement, 4th Edition: McGraw-Hill, New York, 241p.

Temperature correction Factor @ 26°C, Mt = +1.65

ρw@ 26°C=0.99682g/cm3

ηw@ 26°C=0.00874dyn.s/cm2

ρs=2.45g/cm3 from the specific gravity test

Zero Correction Factor, Ro = 1.69

Ms = 24.21 g

Meniscus correction factor, Cm = Hydrometer reading at (top – bottom) of meniscus.

For test # 1,

Cm = 1.0150 – 1.0130 = 0.002

Rh = Rh’ + Cm = 14 + 2 = 16.0

Rd = Rh’ – Ro’ + Cm = 16 – 1.69 + 1.65 = 13.96

Hr = 16.3 – 0.164(16.0) = 16.1333 cm = 161.333 mm

t = 0.50 min = 30sec

D=18ηVg(ρs-ρf)=18(0.00874)(16.1333)980.7(2.45-0.99682)(30)=0.00770cm=0.0770mm

% Finer than D, K%=ρsρs-1RdMs×100=2.452.45-113.9624.21×100=97.43%

Graph of K (%) against D(mm)

From the grading curve,

D60=0.005mm

Conclusion

From the results obtained from the grading curve, it can be stated with certainty that the soil sample is poorly graded.

Experiment 5: COMPACTION TEST

Introduction

Soil compaction is one of the ground improvement techniques in engineering. It is a process in which by expending compactive energy on the soil, the soil grains are made to be more closely rearranged. This increases the shear strength of the soil and reduces its compressibility and permeability. In practice, this will prevent the seepage of water in and out of the soil.

Apparatus

- A cylinder metal mould, Base plate, collar and metal block

- A standard hammer of weight 4.5 kg

- Balance for weighing

- Oven

- Some containers for moisture content

Procedure

- The material provided was sieved through BS test sieve 19 mm.

- 7000g of the sieved material was taken.

- Both the mould and the base plate were weighed.

- The volume of the mould was found with the metal block in it.

- The weighed sample was mixed with water at percentage of ranging 2% to 5% depending upon fines within the material at hand.

- The mould was filled in 5 layers, each layer compacted by 55 blows with hammer, compacted sample was made to be above the height of the mould.

- The soil was trimmed to the height of the mould and the mould and its content weighed.

- Two moisture containers were filled half way with the soil sample and the moisture content determined.

- The process was repeated from step 5 until the mass of the mould and soil started to fall.

Results and Discussion

Table of results

| Mass of cylinder + wet sample(g) | 11681 | 12037 | 12208 | 11909 | 11767 |
| --- | --- | --- | --- | --- | --- |
| Mass of cylinder(g) | 6986 | 6986 | 6986 | 6986 | 6986 |
| Mass of wet sample(g) | 4695 | 5051 | 5222 | 4923 | 4781 |
| Bulk Density(g/cc) | 2.206 | 2.374 | 2.454 | 2.314 | 2.247 |

| Container no. | AT | F4 | AF | KC | E1 | K | E5 | R2 | E16 | YF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mass of container + wet soil(g) | 107.22 | 128.24 | 119.45 | 115.00 | 138.43 | 149.26 | 104.69 | 141.19 | 117.93 | 119.86 |
| Mass of container + dry soil(g) | 98.44 | 119.12 | 106.20 | 107.83 | 123.03 | 133.85 | 93.94 | 124.76 | 105.17 | 105.37 |
| Mass of container(g) | 25.38 | 25.74 | 26.04 | 29.69 | 24.92 | 25.65 | 25.56 | 25.56 | 25.92 | 25.48 |
| Mass of wet soil(g) | 81.84 | 102.50 | 93.41 | 85.31 | 113.51 | 123.61 | 79.13 | 115.63 | 92.01 | 94.38 |
| Mass of dry soil(g) | 73.06 | 93.38 | 80.16 | 78.14 | 98.11 | 108.20 | 68.38 | 99.20 | 79.25 | 79.89 |
| Mass of water(g) | 8.78 | 9.12 | 13.25 | 7.17 | 15.40 | 15.41 | 10.72 | 16.43 | 12.76 | 14.49 |
| Water content(%) | 12.02 | 9.77 | 16.53 | 9.18 | 15.70 | 14.24 | 15.72 | 16.56 | 16.10 | 18.14 |
| Average water content(%) | 10.90 |  | 12.86 |  | 14.97 |  | 16.14 |  | 17.12 |  |
| Dry density (g/cm3) | 1.989 |  | 2.103 |  | 2.134 |  | 1.992 |  | 1.919 |  |

Height of mould, H = 11.65cm

Diameter of mould, D = 15.25cm

Volume of mould, V= πD24×H=2127.921cm3

Calculation

Considering test #1

Bulk density =Mass of wet samplevolume of mould=4695g2127.921cm3=2.206gcm3

Water content =Mass of water Mass of dry soil×100=8.7873.06×100=12.02%

Average water content (%) =12.02+9.762=10.89

Dry density (g/cm3) =Bulk densityAvg. Water content+1=2.2060.1089+1=1.989

A graph of dry density against water content

From the graph,

The maximum dry density = 2.14 g/cm3

The optimum water content occurs at 14.6 %

Conclusion

The maximum dry density and optimum water content of the soil sample are 2.14 g/cm3 and 14.6 % respectively.

Experiment 6: TRIAXIAL TEST

Introduction

During site investigations for buildings; in almost all cases short term stability will be the most critical. The Triaxial test deals with the determination of total shear strength parameters of cohesive soils. The triaxial is the most common method used in soil mechanics laboratory for finding shear strength of the soil.

Apparatus

- 3.8 cm (1.5 inch) internal diameter long sample tubes.

- Rubber ring.

- Moisture content test apparatus.

- A balance

Triaxial machine

Procedure

- The test sample was placed on the Triaxial machine and covered with a rubber membrane with the help of a rubber membrane stretcher. (care was taken to prevent any part of the machine from jogging the sample while it was being setup. E.g. by knocking against the bottom of the loading piston).

- The O-ring was used to tie the rubber membrane at the bottom and top. The setup was covered with a Triaxial cell, and uniformly clamped down to prevent leakage of pressure during the test.

- The cell was filled with water through the breed valve at the top and closed, after ensuring that the cell was well setup.

- The air pressure in the reservoir was increased to raise the hydrostatic pressure in the required amount. (The pressure gauge was critically monitored during the test and necessary adjustments made to keep the pressure constant).

- The handle wheel of the screw jack was rotated until the underside of the hemispherical seating of the proving, through which the loading was applied, just touched the cell piston.

- The piston was then removed down by handle until it just got in touched with the pressure plate on the top of the sample, and the proving ring seating was again brought into contact for the begging of the test.

Results and Discussion

Table of values

| Cell pressure(KPa) |  |  |  | 100 |  | 200 |  | 300 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Change in length (div) | Change in length (mm) | Strain (%) | New area (mm2) | Proving ring reading (div) | Deviator stress, q =σ1-σ3 (KPa) | Proving ring reading (div) | Deviator stress, q =σ1-σ3 (KPa) | Proving ring reading (div) | Deviator stress, q =σ1-σ3 (KPa) |
| 0 | 0.00 | 0.00 | 1134.26 | 0 | 0 | 0 | 0 | 0 | 0 |
| 10 | 0.10 | 0.13 | 1135.75 | 17 | 122 | 5 | 36 | 4 | 29 |
| 20 | 0.20 | 0.26 | 1137.25 | 24 | 172 | 6 | 43 | 7 | 50 |
| 30 | 0.30 | 0.39 | 1138.75 | 30 | 215 | 8 | 57 | 8 | 57 |
| 40 | 0.40 | 0.52 | 1140.25 | 35 | 258 | 9 | 64 | 10 | 72 |
| 50 | 0.50 | 0.66 | 1141.75 | 41 | 293 | 10 | 71 | 11 | 79 |
| 60 | 0.60 | 0.79 | 1143.26 | 45 | 321 | 12 | 86 | 12 | 86 |
| 70 | 0.70 | 0.92 | 1144.78 | 50 | 356 | 13 | 93 | 13 | 93 |
| 80 | 0.80 | 1.05 | 1146.30 | 54 | 384 | 15 | 107 | 14 | 100 |
| 90 | 0.90 | 1.18 | 1147.82 | 59 | 419 | 16 | 114 | 15 | 107 |
| 100 | 1.00 | 1.31 | 1149.35 | 62 | 440 | 16 | 116 | 16 | 114 |
| 120 | 1.20 | 1.57 | 1152.41 | 69 | 489 | 18.5 | 127 | 20 | 142 |
| 140 | 1.40 | 1.84 | 1155.49 | 75 | 530 | 20 | 141 | 36 | 359 |
| 160 | 1.60 | 2.10 | 1158.59 | 81 | 570 | 22 | 155 | 56 | 394 |
| 180 | 1.80 | 2.36 | 1161.70 | 87 | 611 | 24 | 169 | 71 | 499 |
| 200 | 2.00 | 2.62 | 1164.84 | 92 | 644 | 25.5 | 179 | 86 | 602 |
| 250 | 2.50 | 3.28 | 1172.74 | 107 | 745 | 29 | 202 | 117 | 814 |
| 300 | 3.00 | 3.94 | 1180.75 | 117 | 809 | 32.5 | 245 | 144 | 995 |
| 350 | 3.50 | 4.59 | 1188.87 | 127 | 872 | 35.5 | 244 | 167 | 1146 |
| 400 | 4.00 | 5.25 | 1197.10 | 136 | 927 | 39 | 266 | 187 | 1275 |
| 450 | 4.50 | 5.91 | 1205.45 | 143 | 968 | 42 | 284 | 204 | 1380 |
| 500 | 5.00 | 6.56 | 1213.92 | 151 | 1015 | 44.5 | 299 | 220 | 1479 |
| 550 | 5.50 | 7.22 | 1222.50 | 156 | 1041 | 47 | 314 | 234 | 1562 |
| 600 | 6.00 | 7.87 | 1231.21 | 166 | 1100 | 49.5 | 328 | 242 | 1604 |
| 700 | 7.00 | 9.19 | 1249.00 | 175 | 1143 | 53.5 | 350 | 271 | 1771 |
| 800 | 8.00 | 10.50 | 1267.31 | 176 | 1133 | 57.5 | 370 | 291 | 1874 |
| 900 | 9.00 | 11.81 | 1286.17 | 174 | 1104 | 60.3 | 383 | 301 | 1960 |
| 1000 | 10.00 | 13.12 | 1305.60 | 170 | 1063 | 63 | 394 | 324 | 2025 |
| 1100 | 11.00 | 14.44 | 1325.63 | 168 | 1034 | 65 | 400 | 334 | 2056 |
| 1200 | 12.00 | 15.75 | 1346.27 | 166 | 1006 | 67 | 406 | 340 | 2060 |
| 1300 | 13.00 | 17.06 | 1367.58 | 164 | 979 | 69 | 412 | 342 | 2041 |
| 1400 | 14.00 | 18.37 | 1389.56 | 162 | 951 | 70.2 | 412 | 343 | 2014 |
| 1500 | 15.00 | 19.69 | 1412.27 | 161 | 930 | 72 | 410 | 340 | 1964 |
| 1600 | 16.00 | 21.00 | 1435.73 | 160 | 909 | 71.8 | 408 | 340 | 1932 |

| Test | Cell pressure σ3/kPa | Deviator stress (kPa) | Maximum Principal stress σ1/kPa | Centre kPa | Radius kPa |
| --- | --- | --- | --- | --- | --- |
| 1 | 100 | 1143 | 1243 | 671.5 | 571.5 |
| 2 | 200 | 412 | 612 | 406 | 206 |
| 3 | 300 | 2060 | 2360 | 1330 | 1030 |

τ=c+ σ tanφ

From the mohr circle drawn;

φ=47.5°

C = 120KPa

Therefore at the maximum principal stress, σ1=2360KPa,

τ= 120 + 2360 tan (47.5°) = 2695.49 KPa

Conclusion

The shear strength of the soil sample used was calculated with the help of graphs and found out to be 2695.49 KPa. Errors may be due parallax in reading of experimental values and machine deficiency.

GENERAL CONCLUSION

In conclusion, it can be stated that from the results obtained from both the hydrometer analysis and the particle sizes distribution test in terms of coefficient of uniformity and coefficient of curvature, the soil sample provided can be classified under poorly graded.

Also from results obtained from both the plastic and liquid limit tests, it can also be said that there are appreciable errors incurred during the experiment. Hence a deviation of results from the properties of soil under engineering behaviour. We also appreciated the fact that the soil reflects characteristics of engineering behavior under natural uninterrupted situations in the field.

With respect to the specific gravity test, it can be concluded that a soil with Specific gravity of 2.45 is free from organic matter and porous particles. Hence the soil sample exhibit these properties.

REFERENCES

- Prof. S.K. Agodzo, KNUST, soil mechanics application to mechanization.

- Bowles, J.E.1992, Engineering Properties of Soils and Their Measurement, 4th Edition: McGraw-Hill, New York, 241p.